# Gold Biorecovery from E-Waste — Combined Modelling Document

Bioleaching · GolB Surface Display · Capture, Elution, Reduction, Recovery

2026-08-09

Table of Contents

# About this document

This is a compilation of three modelling documents that together describe one process chain, from crushed printed circuit boards to recovered metallic gold.

The three source documents are reproduced verbatim. Nothing has been deleted, reworded, corrected, or renumbered. Where the sources disagree with each other, or contain an apparent error, the disagreement is recorded in ISSUES.md and left standing in the text.

| Part | Source file | Stage of the chain |
| --- | --- | --- |
| I | Bioleaching Models.docx | Leaching — PCB → dissolved Au(S₂O₃)₂³⁻ |
| II | GolB_model_writeup.docx | Expression — GolB surface site density |
| III | model.md v3.0 | Capture → elution → reduction → recovery |

Pristine copies of all three originals are kept in docs/source/.

## The chain

crushed PCB
      │
      │  PART I — Bioleaching (TetH → thiosulfate → Au/Cu leaching)
      ▼
  leachate:  [Au(S2O3)2 3-],  [Cu(I)],  [Cu(II)],  [S2O3 2-]
      │
      │  ══ JOINT 1 ══  Au_feed
      ▼
  PART III §2 — V1 capture on GolB-displaying E. coli
      ▲
      │  ══ JOINT 2 ══  q_max
      │
  PART II — GolB expression cascade (mRNA → Pc → Ps → active sites A)

  PART III continues:  capture → elution → reduction → recovery → eta_total

## The two joints

The three models are not three separate topics. Two named quantities connect them, and each is a quantity that one document declares missing and another document supplies.

Joint 1 — Au_feed. Part III §10 states: “Au_feed has no upstream model though it dominates V1.” Part I computes exactly that quantity as [Au(S₂O₃)₂³⁻](t). Adapter: src/interfaces.py :: au_feed_from_leach.

Joint 2 — q_max. Part III §9 ranks q_max as measurement priority 2 and notes it is “being addressed by the secretion model.” Part II §5 computes the active-site count A* per cell, which converts to q_max in µM/(g/L). Adapter: src/interfaces.py :: qmax_from_expression.

## Unit systems in use

The three documents were written in different unit systems. They are not harmonised in the text below. Conversion happens once, inside the adapters.

| Part | Concentration | Time | Amount |
| --- | --- | --- | --- |
| I — Bioleaching | µmol L⁻¹ | minutes | µmol, mol |
| II — Expression | molecules/cell | minutes | molecules |
| III — Recovery chain | µM | hours | µM, g/L |

Note that µmol L⁻¹ and µM are the same unit under two names. Time is not the same: Part I and Part II are per-minute, Part III is per-hour.

## Validation status

Part III §0 opens with a statement that governs the whole compilation:

No part of this model has been checked against a measurement of this system.

That statement was written about Part III. It applies at least as strongly to Parts I and II, whose parameter tables carry the entries calibrate, unmeasured, fitted, assumed, and placeholder.

# Part I — Bioleaching Model

Source: Bioleaching Models.docx. Reproduced verbatim.

# Bioleaching Modelling — Process Overview

Bacteria express tetrathionate hydrolase (TetH), which breaks tetrathionate down into thiosulfate. The thiosulfate then leaches gold (and, unavoidably, copper) from crushed PCB particles. The chain of models is:

- Enzyme production rate

- Tetrathionate consumption rate

- Thiosulfate production rate (with Cu(II) coupling)

- Gold leaching rate — Model A (oxygen only) and Model B (oxygen + Cu(II))

- Copper leaching rate and the Cu(I)/Cu(II) balance

- pH change (to be built)

## Enzyme Production

Bacteria produce tetrathionate hydrolase (TetH), which hydrolyses tetrathionate to thiosulfate.[1]

Reaction

bacteria → TetH enzyme (E)

Model

Enzyme concentration is governed by three processes — production (proportional to biomass), first-order degradation, and dilution as the cells grow [3]:

d[E]dt= ksyn⋅X  −  (kdeg+μ)⋅E

At steady state, [E]ₛₛ = k_syn·X / (k_deg + μ), reached over a characteristic time of 1/(k_deg+μ) [3]. Under the fixed-biomass assumption (no growth), μ = 0.

Parameters

| Symbol | Meaning | Unit | Value / source |
| --- | --- | --- | --- |
| [E] | Active TetH concentration | µmol L⁻¹ | state variable |
| t | Time | min | — |
| X | Biomass concentration | cell L⁻¹ | input / measured |
| k_syn | Enzyme synthesis rate per cell | µmol cell⁻¹ min⁻¹ | calibrate |
| k_deg | Enzyme degradation rate | min⁻¹ | ≈1.1×10⁻³ [4] |
| Μ | Growth-dilution rate (=ln2/t_double) | min⁻¹ | 0 if no growth [3] |

## Tetrathionate Consumption

Reactions

TetH hydrolyses tetrathionate via a disulfane-monosulfonic-acid (DSMSA) intermediate [1]:

S₄O₆²⁻ + H₂O → HS₂SO₃⁻ + HSO₄⁻

HS₂SO₃⁻ → S₂O₃²⁻ + S⁰ + H⁺

Lumped into a single overall reaction:

S₄O₆²⁻ + H₂O → S₂O₃²⁻ + S⁰ + SO₄²⁻ + 2H⁺

Copper(II) leached from the PCB re-oxidises thiosulfate back to tetrathionate, so a regeneration term is required [6][7]:

2Cu(II) + 2S₂O₃²⁻ → 2Cu(I) + S₄O₆²⁻

Model

Consumption follows irreversible Michaelis–Menten kinetics [5]; the parasitic reaction above adds tetrathionate back:

dS4O62−dt= Fin−kcat⋅E⋅S4O62−Km+ S4O62−+ k₁⋅[Cu(II)]⋅[S₂O₃²⁻]

Parameters

| Symbol | Meaning | Unit | Value / source |
| --- | --- | --- | --- |
| [S₄O₆²⁻] | Tetrathionate concentration | µmol L⁻¹ | state variable |
| F_in | Tetrathionate feed rate | µmol L⁻¹ min⁻¹ | operating choice |
| k_cat | Turnover number of TetH | min⁻¹ | unmeasured — calibrate [1] |
| K_m | Michaelis constant | µmol L⁻¹ | 50–2400 [2] |
| E | Active TetH concentration | µmol L⁻¹ | from Section 1 |
| k₁ | Parasitic Cu(II)–thiosulfate rate constant | L µmol⁻¹ min⁻¹ | calibrate (↑ w/o NH₃) [6][7] |
| [Cu(II)] | Copper(II) concentration | µmol L⁻¹ | from Section 5 |

# Thiosulfate Production

Thiosulfate is produced as a stoichiometric multiple (Y) of tetrathionate consumed.

dS2O32−dt=kcat⋅E⋅S4O62−Km+ S4O62− [production only]

Adding the parasitic loss to Cu(II) (2 thiosulfate consumed per reaction extent) and the loss to gold leaching gives the full balance:

dS2O32−dt  =kcat⋅E⋅S4O62−Km+S4O62−−2⋅k1⋅Cu(II)⋅S2O32−−2V⋅RAu−1V⋅RCu

where R_Au is the gold-leaching rate (µmol min⁻¹) and R_Cu is the copper-leaching rate (µmol min⁻¹) from Sections 4 and 5. Each gold atom consumes 2 thiosulfate, and, depending on the oxidant, each copper atom consumes 2 or 4 thiosulfate. The 1/V converts the surface rate to a concentration rate.

Parameters

| Symbol | Meaning | Unit | Value / source |
| --- | --- | --- | --- |
| [S₂O₃²⁻] | Thiosulfate concentration | µmol L⁻¹ | state variable |
| Y | Stoichiometric yield (S₂O₃ per S₄O₆) | — (dimensionless) | 1 [1] |
| V | Reactor volume | L | operating choice |
| R_Au | Gold leaching rate | µmol min⁻¹ | from Section 4 |
| R_Cu | Copper leaching rate | µmol min⁻¹ | From Section 5 |

# Gold Leaching

Reactions

Metallic gold is oxidised and complexed by thiosulfate. The oxidation and complexation happen in a single surface step (free Au⁺ does not persist in solution) [8]:

Au⁰ + 2S₂O₃²⁻ → Au(S₂O₃)₂³⁻ + e⁻ (anodic half-reaction)

With oxygen as the terminal oxidant, the overall reaction is:

4Au⁰ + 8S₂O₃²⁻ + O₂ + 2H₂O → 4Au(S₂O₃)₂³⁻ + 4OH⁻

Because copper is leached from the PCB, a second, faster pathway exists in which Cu(II) is the oxidant [11][12]:

Au⁰ + 2S₂O₃²⁻ + Cu(II) → Au(S₂O₃)₂³⁻ + Cu(I)

Gold Surface-Area Equation

Gold on a PCB is a thin plated film, not a bulk particle, so it dissolves by thinning at roughly constant face area until it is exhausted (it does not shrink inward). The exposed area is fixed by the gold mass and plating thickness, independent of how finely the board is crushed:

AAu =mAuρAu ⋅ tfilm

$A_{Au} (t)   A_{Au}(0) $while gold remains, → 0 once exhausted

Derivation: a film of area A and thickness t has volume A·t = m/ρ, so A = m/(ρ·t).

### Model A — Oxygen only (conservative)

Starting from simple mass action, gold leaching depends on oxygen (oxidant) and thiosulfate (ligand). Because gold sits on the particle surface, the rate scales with a time-dependent gold area — a shrinking-surface variant of the shrinking-core model

Since the surface has a finite number of reaction sites, each reactant enters through a saturating (Langmuir) term [8][10]. Tracking solid gold in mol and dissolved gold as a concentration:

RAu = kAu,O2⋅ AAu(t)⋅O2KO2+O2 ⋅S2O32−KS+S2O32−

dnAudt= − RAu

dAuS2O323−dt=+RAuV

### Model B — Oxygen + Copper(II) (realistic)

Cu(II) provides a parallel oxidant pathway. Parallel pathways add (either oxidant alone can dissolve gold), while area, thiosulfate, and passivation multiply everything (all are required regardless of oxidant). Oxygen enters only its own term — Cu(II) does not need O₂ at the gold surface [15]:

RAu = AAu(t)⋅S2O32−KS+S2O32−  ⋅ {kAu,O2⋅O2KO2+O2 + kAu,Cu⋅Cu(II)KCu+Cu(II) }

dnAudt = −RAu

dAuO33−dt = +RAuV

Parameters

| Symbol | Meaning | Unit | Value / Source |
| --- | --- | --- | --- |
| n_Au | Solid gold remaining | mol (or µmol) | state variable |
| [Au(S₂O₃)₂³⁻] | Dissolved gold complex (product) | µmol L⁻¹ | state variable |
| A_Au | Exposed gold area = m_Au/(ρ_Au·t_film) | m² | from geometry |
| ρ_Au | Gold density | kg m⁻³ | 19300 |
| t_film | Gold plating thickness | M | 0.05–1 ×10⁻⁶ (board spec) |
| k_Au,O₂ | Gold rate constant, O₂ route | µmol m⁻² min⁻¹ | ≈11 (1.9×10⁻⁷ mol m⁻²s⁻¹) [9][10] |
| k_Au,Cu | Gold rate constant, Cu(II) route | µmol m⁻² min⁻¹ | ≈10³× larger [11][12] |
| K_O₂ | O₂ half-saturation | µmol L⁻¹ | calibrate (~50) |
| K_S | Thiosulfate half-saturation | µmol L⁻¹ | calibrate (~5×10⁴) |
| K_Cu | Cu(II) half-saturation | µmol L⁻¹ | Calibrate |

## Copper Leaching and the Cu(I)/Cu(II) Balance

Reactions

Metallic copper dissolves as Cu(I)–thiosulfate. Two oxidant pathways exist [13][7]:

With oxygen as oxidant:

4Cu⁰ + O₂ + 8S₂O₃²⁻ + 2H₂O → 4[Cu(S₂O₃)₂]³⁻ + 4OH⁻

With Cu(II) as oxidant (comproportionating one Cu(II) plus one Cu⁰ gives two Cu(I)):

Cu⁰ + Cu²⁺ → 2Cu⁺

Cu⁺ + 2S₂O₃²⁻ → [Cu(S₂O₃)₂]³⁻

Cu⁰ + Cu²⁺ + 4S₂O₃²⁻ → 2[Cu(S₂O₃)₂]³⁻

Cu(I) is re-oxidised to Cu(II) by oxygen, and Cu(II) is reduced back to Cu(I) by thiosulfate and by gold leaching [7][15]:

4Cu(I) + O₂ + 2H₂O → 4Cu(II) + 4OH⁻

2Cu(II) + 2S₂O₃²⁻ → 2Cu(I) + S₄O₆²⁻

Au⁰ + 2S₂O₃²⁻ + Cu(II) → Au(S₂O₃)₂³⁻ + Cu(I)

Copper Surface-Area Equation

Copper is bulk metal (traces, planes, inner layers), so its particles genuinely erode inward — a true shrinking-particle geometry

The initial area follows the surface-to-volume ratio 6/d for crushed particles of size d; as copper is consumed, the area falls as the two-thirds power of the fraction remaining (area ∝ r², volume ∝ r³) [14]:

ACu(0)= 6⋅mCu(ρCu ⋅ d)

ACu(t) = ACu(0) ⋅ nCunCu(0)23

Rates

Copper leaching, oxygen route (v₁A) and combined-oxidant route (v₁B); gold-leaching Cu(I) return (v₂); parasitic tetrathionate regeneration (v₃); Cu(I) re-oxidation by oxygen (v₄):

v1A = 2kCu,O2⋅ACu(t)⋅O2KO2+O2⋅S2O32−KS+S2O32−

v1B = ACu(t)⋅S2O32−KS+S2O32−⋅{ 2kCu,O2⋅O2KO2+O2 + 4kCu,  Cu2+⋅Cu(II)KCu+Cu(II) }

v₂ = RAu  (gold−leaching rate, Section 4)

v₃ = k₃⋅[Cu(II)]⋅[S₂O₃²⁻]

v₄ = k₄⋅[O₂]⋅[Cu(I)]

Cu(I) model

Cu(I) is produced by copper leaching, by gold leaching, and by the parasitic reaction, and is consumed by oxygen re-oxidation. Reading coefficients off the balanced reactions (comproportionating gives 2 Cu(I) per extent; parasitic gives 2 Cu(I) per extent; O₂ re-oxidation consumes 4 Cu(I) per extent):

dCu(I)dt = 1V⋅2⋅v₁B + 1V⋅v₂ + 2⋅v₃ − 4⋅v₄

Cu(II) model

Cu(II) is produced only by oxygen re-oxidation of Cu(I), and consumed by the comproportionating leach, the parasitic reaction, and gold leaching:

dCu(II)dt = 4⋅v₄ − 1V⋅v₁B − 1V⋅v₂ − 2⋅v₃

Parameters

| Symbol | Meaning | Unit | Value / source |
| --- | --- | --- | --- |
| [Cu(I)] | Copper(I) concentration (cannot leach gold) | µmol L⁻¹ | state variable |
| [Cu(II)] | Copper(II) concentration (gold oxidant) | µmol L⁻¹ | state variable |
| n_Cu | Solid copper remaining | mol | state variable |
| A_Cu | Exposed copper area = 6m_Cu/(ρ_Cu·d)·(n/n₀)^⅔ | m² | from geometry |
| ρ_Cu | Copper density | kg m⁻³ | 8960 |
| d | Crushed particle size | m | 2–6×10⁻³ (your feed) |
| k_Cu,O₂ | Copper rate constant, O₂ route | µmol m⁻² min⁻¹ | calibrate (Ea≈25.8 kJ/mol) [13] |
| k_Cu,Cu | Copper rate constant, Cu(II) route | µmol m⁻² min⁻¹ | calibrate |
| k₃ | Parasitic (Cu(II)+S₂O₃) rate constant | L µmol⁻¹ min⁻¹ | ≈ k₁ [6][7] |
| k₄ | Cu(I) re-oxidation rate constant | L µmol⁻¹ min⁻¹ | calibrate |

# References

[1] Y. Kanao et al., "Tetrathionate hydrolase from the acidophilic microorganisms," Front. Microbiol., vol. 15, 1338669, 2024.

[2] Y. Kanao, K. Kamimura, and T. Sugio, "Purification of a tetrathionate hydrolase from Acidithiobacillus ferrooxidans," J. Biotechnol., vol. 132, pp. 16–22, 2007.

[3] U. Alon, An Introduction to Systems Biology, 2nd ed. Boca Raton, FL: CRC Press, 2019.

[4] M. R. Maurizi, "Proteases and protein degradation in Escherichia coli," Experientia, vol. 48, pp. 178–201, 1992.

[5] G. E. Briggs and J. B. S. Haldane, "A note on the kinetics of enzyme action," Biochem. J., vol. 19, pp. 338–339, 1925.

[6] J. J. Byerley, S. A. Fouda, and G. L. Rempel, "Kinetics and mechanism of the oxidation of thiosulphate ions by copper(II) ions in aqueous ammonia solution," J. Chem. Soc. Dalton Trans., pp. 889–893, 1973.

[7] P. L. Breuer and M. I. Jeffrey, "The reduction of copper(II) and the oxidation of thiosulfate and oxysulfur anions in gold leaching solutions," Hydrometallurgy, vol. 70, pp. 163–173, 2003.

[8] G. Senanayake, "Analysis of reaction kinetics, speciation and mechanism of gold leaching and thiosulfate oxidation by ammoniacal copper(II) solutions," Hydrometallurgy, vol. 75, pp. 55–75, 2004.

[9] S. Zhang and M. J. Nicol, "An electrochemical study of the dissolution of gold in thiosulfate solutions Part I: Alkaline solutions," J. Appl. Electrochem., vol. 33, pp. 767–775, 2003.

[10] O. Sitando et al., "A review of factors affecting gold leaching in non-ammoniacal thiosulfate solutions," Hydrometallurgy, vol. 178, pp. 151–175, 2018.

[11] M. G. Aylmore and D. M. Muir, "Thiosulfate leaching of gold — a review," Miner. Eng., vol. 14, no. 2, pp. 135–174, 2001.

[12] D. Maharaj, T. Moyo, and J. Petersen, "Ammonium thiosulfate leaching of gold from electronic printed circuit boards — effect of solution copper concentration," J. S. Afr. Inst. Min. Metall., vol. 124, no. 12, pp. 711–718, 2024.

[13] E. Salinas-Rodríguez et al., "Leaching of copper contained in waste printed circuit boards using the thiosulfate–oxygen system: a kinetic approach," Materials, vol. 15, no. 7, 2354, 2022.

[14] O. Levenspiel, Chemical Reaction Engineering, 3rd ed. New York, NY: Wiley, 1999.

[15] P. L. Breuer and M. I. Jeffrey, "The effect of ionic strength and buffer choice on the decomposition of tetrathionate; and the role of copper(II) as oxidant in gold thiosulfate leaching," Hydrometallurgy, vol. 65, pp. 145–157, 2002.

# Part II — GolB Surface Site Density Model

Source: GolB_model_writeup.docx. Reproduced verbatim; figure paths repointed to docs/media/.

Modeling Surface Site Density for GolB-Based Gold Biosorption

# 1. Purpose and scope

Our project recovers gold from electronic waste in two stages: bioleaching mobilizes gold from the waste into a leachate, and biosorption then captures the dissolved gold using engineered bacteria. For biosorption we display the gold-binding protein GolB on the cell surface, so that gold ions in the leachate bind directly to accessible protein rather than having to enter the cell. The quantity that determines how much gold a single cell can capture is the surface site density — the number of active, gold-accessible GolB molecules on the outer membrane.

This model predicts that surface site density from first principles, tracing the gene-expression cascade that produces it: transcription of the GolB gene into mRNA, translation into cytoplasmic protein, export and anchoring of that protein at the surface, and finally the fraction of surface protein that is correctly folded and able to bind gold. Because our team works from published data rather than our own measurements, every parameter is a literature-grounded estimate, and the two parameters that cannot be read directly from the literature are treated as explicitly fitted values.

# 2. Model structure

We represent the system as four connected pools, expressed as molecules per cell. Each pool is fed by the process upstream of it and drained by degradation and by dilution as the cell grows and divides:

mRNA m → cytoplasmic protein Pc → surface-displayed protein Ps → active sites A

Dilution appears because a growing cell continually doubles its volume; even a perfectly stable protein is diluted at the growth rate. For fast-turnover species such as mRNA this term is small, but for stable proteins it is often the dominant loss.

# 3. Governing equations

The cascade is written as a system of ordinary differential equations. Transcription produces mRNA at a rate set by promoter strength and copy number, and mRNA is lost to degradation and dilution:

dm/dt = α·N − (δm + μ)·m

Translation converts each mRNA into protein; the cytoplasmic pool is drained by export to the surface, by degradation, and by dilution:

dPc/dt = β·m − (k_sec + δc + μ)·Pc

Export anchors protein at the surface. Because the membrane holds a finite number of anchors, the arrival term saturates as the surface fills toward its capacity:

dPs/dt = k_sec·Pc·(1 − Ps/Ps,max) − (δs + μ)·Ps

Finally, only a fraction of the displayed protein is correctly folded and gold-accessible, so the number of active binding sites is:

A = f·Ps

# 4. Parameters

The table below lists every parameter, the value used in the simulation, and its basis in the literature. The central-dogma constants are standard order-of-magnitude values for Escherichia coli. The surface capacity comes from characterized autodisplay systems. Two parameters — the display rate k_sec and the functional fraction f — depend on the specific construct and are treated as fitted; the gold dissociation constant K_d is a placeholder because no clean experimental value for GolB has been reported.

| Symbol | Meaning | Value | Units | Basis / source |
| --- | --- | --- | --- | --- |
| α | Transcription rate per plasmid copy (promoter strength) | 0.5 | mRNA·min⁻¹·copy⁻¹ | Typical E. coli promoter output (BioNumbers) |
| N | Plasmid copy number | 20 | copies/cell | Medium-copy backbone, pBR322-like (≈15–20) |
| δₘ | mRNA degradation rate | 0.20 | min⁻¹ | E. coli mRNA half-life ≈2–5 min (t½≈3.5 min) |
| β | Translation rate per mRNA (RBS strength) | 4.0 | protein·min⁻¹·mRNA⁻¹ | Typical E. coli translation efficiency (BioNumbers) |
| k_sec | Export / surface-display rate constant | 0.10 | min⁻¹ | Set by the display scaffold; fitted parameter |
| δ_c | Cytoplasmic protein degradation | 0.005 | min⁻¹ | ≈0 for a stable protein |
| δ_s | Surface protein loss | 0.005 | min⁻¹ | Assumed dilution-dominated |
| μ | Growth (dilution) rate | 0.02 | min⁻¹ | Doubling time ≈35 min (μ = ln2 / t_double) |
| f | Fraction folded + gold-accessible | 0.5 | – | Folding/accessibility; fitted parameter |
| P_s,max | Maximum surface anchor sites | 1×10⁵ | sites/cell | Autodisplay reaches >10⁵ molecules/cell (Jose & Meyer) |
| K_d | GolB–Au(I) dissociation constant | 10 | µM | Placeholder – no clean experimental K_d; source or fit |

# 5. Steady-state site density

Setting the time derivatives to zero and substituting down the cascade gives closed-form steady-state values (in the non-saturating limit, valid whenever site density stays well below capacity, which holds here):

m* = αN / (δm + μ)

Pc* = βm* / (k_sec + δc + μ)

Ps* = k_secPc* / (δs + μ)

Combining these yields a single expression for the quantity we care about:

A* = f·α·N·β·k_sec / [(δm + μ)(k_sec + δc + μ)(δs + μ)]

This makes the design logic explicit: site density scales linearly with promoter strength, copy number, and translation strength, while the secretion rate partitions protein between the cytoplasm and the surface. With the parameters above, the model gives roughly 45 mRNA, 1,460 cytoplasmic protein, 5,500 surface protein, and about 2,900 active sites per cell.

# 6. Coupling to gold uptake

The active-site count feeds a Langmuir adsorption isotherm that predicts how much gold a cell binds at a given leachate concentration C. Because GolB binds Au(I) through a single Cys-X-X-Cys motif, each site captures one gold ion, so the maximum uptake equals the site count A:

q(C) = A·C / (Kd + C)

This is the bridge between the expression model and the actual objective: whatever raises the active-site count raises the recovery ceiling proportionally.

# 7. Simulation results

Figure 1 shows the model run to steady state and two analyses derived from it.

Figure 1. (a) Transcript dynamics; (b) protein and active-site dynamics; (c) steady-state site density versus display rate; (d) normalized parameter sensitivity of the steady-state site density.

Panel (a) — Transcript dynamics. mRNA reaches steady state (about 45 copies per cell) within roughly 20–30 minutes. This is fast because mRNA turns over quickly; a species equilibrates on the timescale of a few of its own half-lives, and mRNA half-life is only a few minutes.

Panel (b) — Protein and active sites. The cytoplasmic pool (≈1,460), the surface pool (≈5,500), and the active sites (≈2,900, being half the surface pool) rise much more slowly, taking around 150–200 minutes to plateau. The slowness comes from the protein loss being dominated by dilution, which is far slower than mRNA turnover. Notably the surface pool exceeds the cytoplasmic pool: export continuously drains the cytoplasm, whereas the surface pool is lost only to slow dilution, so displayed protein accumulates.

Panel (c) — Sensitivity to display rate. Steady-state site density is plotted against the export rate k_sec on a logarithmic axis, giving an S-shaped curve. When export is slow, protein remains trapped in the cytoplasm and few sites form. As export speeds up, more protein reaches the surface, but above roughly 1 min⁻¹ the curve flattens near 3,600 sites because transcription and translation, not export, now set the ceiling. The marked point is the operating value used (0.1 min⁻¹). The practical message is that simply making secretion faster yields diminishing returns.

Panel (d) — Which parameter moves site density. Each bar is a normalized sensitivity: the fractional change in steady-state site density per fractional change in that parameter. Promoter strength (α), copy number (N), translation strength (β), and functional fraction (f) all sit near +1, meaning a 1% increase in any of them gives about a 1% increase in sites — these are the highest-leverage engineering handles. The export rate k_sec is only about +0.2 (sublinear, because it appears in both the numerator and a denominator), confirming the diminishing returns seen in panel (c). Growth rate (μ) is the strongest negative influence because it appears in all three loss terms, and mRNA degradation (δₘ) is also strongly negative; cytoplasmic and surface degradation matter little at these values.

Figure 2 translates site density into predicted gold capture.

Figure 2. Langmuir uptake curves for three engineered site densities (base, 2×, and 5×), showing gold ions bound per cell as a function of leachate Au(I) concentration.

Each curve rises with leachate gold concentration and plateaus at its own site density — the plateau is simply the number of sites, since each binds one ion. The three curves correspond to the base design (≈2,900 sites) and to two- and five-fold improvements. Half-saturation occurs at a concentration equal to Kd (10 µM here), and above roughly 100 µM every design is near saturation. The key takeaway is that at any fixed leachate concentration, gold captured scales directly with engineered site density, so the expression-level improvements identified in Figure 1 carry straight through to recovery capacity.

# 8. Assumptions and limitations

The model is deterministic and describes an average cell, so it does not capture cell-to-cell variability. Expression is treated as constant and constitutive; induction timing, resource competition, and the growth burden of heavy membrane-protein overexpression are not included. The drain on the cytoplasmic pool is kept first-order so that a closed-form steady state exists, with saturation applied only to surface arrival; this is accurate while site density stays well below capacity, which is the case here (thousands of sites against a ceiling of 10⁵). Finally, the parameters are literature order-of-magnitude estimates rather than measurements of our exact construct, and the gold dissociation constant in particular is a placeholder that should be sourced from a biosorption isotherm or fitted.

# 9. Literature basis

Surface-display capacity. Jose J, Meyer TF. Autodisplay: efficient bacterial surface display of recombinant proteins. Applied Microbiology and Biotechnology (2006) — reports more than 10⁵ recombinant molecules displayed per cell via the AIDA-I autotransporter.

GolB structure and gold binding. Structural Insights and the Surprisingly Low Mechanical Stability of the Au–S Bond in the Gold-Specific Protein GolB. Journal of the American Chemical Society (2015) — apo- and Au(I)-bound GolB crystal structures and the Cys-X-X-Cys binding motif. Tolbatov I, Re N, Coletti C, Marrone A. An Insight on the Gold(I) Affinity of golB Protein via Multilevel Computational Approaches (2019).

Gold sensing and the gol system. Bacterial gold sensing and resistance. BioMetals (2011) — GolS/GolB selectivity for Au(I). GolS controls the response to gold by hierarchical induction of Salmonella-specific genes. Molecular Microbiology (2007) — GolB as a small cytoplasmic gold-binding protein.

Prior GolB display precedent. iGEM Registry part BBa_K1701000 — GolB displayed on the E. coli surface for selective enrichment of gold ions from mixed-metal media (parts.igem.org).

Central-dogma parameters. BioNumbers database (bionumbers.hms.harvard.edu) for E. coli mRNA half-lives, translation rates, and growth rates.

# Part III — Gold Biorecovery Model v3.0

Source: model.md v3.0 (2026-08-04). Reproduced verbatim.

# Gold Biorecovery — Model

v3.0 (2026-08-04) · Code: pipeline_model.py, r9L_fw.py, ensemble.py Units: µM, hours, g/L · Companion: build plan v2.5 (decisions, audit trail, citations)

This document is current state only. Change history, superseded results and provenance disputes live in the build plan.

## 0. Validation status — read first

No part of this model has been checked against a measurement of this system. Every parameter is literature-transplanted, proxy-bounded, or declared. The verification checks confirm the code solves the equations; they say nothing about whether the equations describe reality.

Three facts bound every claim below:

- No demonstration exists that this construct reduces gold in a lysate. The source paper used purified protein + added dithionite on pure HAuCl₄; the process uses crude lysate + native reductants on thiourea eluate.

- Conversion has never been quantified by anyone, in any version of this chemistry. Both source papers detect product by colour and TEM only.

- Selectivity against Cu/Ag/Ni is unknown. Both source papers used pure gold.

The deliverable is a ranked measurement priority list, not a yield prediction.

Track record: every parameter assumed without a source, then sourced, was wrong — A_tox (wrong regime), K_D (≥12 orders), k_red (7×), eta_spin (2×). eta_wash is the last unsourced parameter and should be treated as an upper bound.

## 1. The chain

ηtotal=ηcapture⋅ηelute⋅ηreduce⋅ηphys

Two parallel arms converge at reduction:

ARM A (gold)                              ARM B (reagent)
  leach (out of scope) → sets Au_feed       grow E. coli BL21 + ABC construct
        ↓                                   induce 1 mM IPTG, 4 h
  V1 capture biofilm, 13-16 h               lyse: sonicate, 100,000 g 90 min
        ↓ thiourea elution, 3 h                    ↓
  conditioning (not modelled) ──────→  V2 lysate reduction, 12-24 h, pH 7.4
                                              ↓
                                       recovery: spin → wash → ash

Critical path ≈ 42 h/batch. Conditioning is the only unmodelled series step (assumed lossless).

Current: eta_total = 10.5% median, 90% CI [0.0%, 49.4%].

## 2. V1 — capture

Living E. coli displaying GolB in an LB-like (chelating) medium. States: X biomass, C bound gold, D damage.

A=Autot−C  S0=qmaxX  G=A+wC

dXdt=μX1−XXmax−mX−λDDX

dCdt=konA(S0−C)−koffC

dDdt=kdamG−krepD  λD=μkrep0Atox

Lethality is pinned to a fixed value rather than scaled with repair, so slow repair appears as harm rather than compensation.

Verification (all pass): Langmuir limit (Ceq=S0A/(A+KD), err 2e-09); binding half-time; gold mass balance; zero-gold logistic limit; capacity ceiling η≤qmaxXmax/Autot.

### 2.1 Two results that matter

No harvest-time optimum exists. In an LB-like medium at sub-onset feed, capture is flat: 79.5% at 12 h, 79.8% at 24 h, 79.7% at 72 h. Harvest any time after ~12 h. The earlier “toxicity racing binding” result was an artefact of a buffer-regime A_tox.

Au_feed is the dominant design variable, and an input from the out-of-scope leaching model:

| Au_feed | η (A_tox=250) | η (A_tox=30) | Au captured | limited by |
| --- | --- | --- | --- | --- |
| 3 µM | 85.2% | 84.2% | 2.56 µM | equilibrium |
| 10 µM | 79.9% | 73.3% | 7.99 µM | equilibrium |
| 22 µM | 64.8% | 37.7% | 14.26 µM | ← transition |
| 50 µM | 33.7% | 4.1% | 16.84 µM (peak) | capacity |
| 300 µM | 1.6% | 0.1% | 4.70 µM | capacity |

The transition is exactly the capacity ceiling qmaxXmax = 22 µM. Absolute capture peaks near 50 µM feed but that is where A_tox uncertainty swings capture ~8×.

Recommended operating point: 10–20 µM feed — below the absolute peak, but the A_tox disagreement costs <10% there vs 63–96% above 30 µM. Dilution is a legitimate design lever.

Capture is capacity-limited, not affinity-limited. At 10 µM feed, sites must exceed 10 µM, requiring X > 2.27 g/L.

## 3. Elution

Mechanism: thiourea competitive ligand exchange, not acid. One Au atom is chelated between two sulfur atoms of two thiourea molecules — a better bidentate site than GolB’s Cys10/Cys13. Acid (pH 1.4–1.8) is a co-requirement, not the mechanism.

⚠️ The project architecture assumed an acid wash. If the wet lab plans acid-only, elution may recover far less than (1−ϕ) predicts and the model would not show it — k_max is a fitted rate that silently absorbs “the eluent doesn’t work.” Confirm the eluent.

Thiourea at ~1 M against micromolar gold is a ~10⁴ excess, so the exchange is pseudo-first-order:

dCdt=−k[TU]n⏟kmax(C−ϕC0)+

ηelute(tk)=(1−ϕ)1−e−kmaxtk

- (1−ϕ) — ceiling. Chemistry. Not improvable by time or acid strength.

- (1−e−kmaxtk) — approach. 95% of ceiling at 3/kmax.

Different fixes: a short wash is cured by patience; a low ceiling is not. Sampling at 0.5/1/2/4 h distinguishes them.

pKa_GolB and n_H leave the model — below pH 2 the thiourea route is fully open.

k_max is a design lever since kmax=k[TU]n: at 2 M the wash finishes in an hour; at 0.1 M six hours is not enough.

## 4. Reduction (rung 9L)

Cell-free metabolic engineering with crude extract. The protein is a stoichiometric redox reactant, not a catalyst — one exterior Cys337–Cys481 disulfide, 2 electrons, consumed per use.

Crude lysate reduces gold with no added reductant (published); only purified protein needs dithionite, because purification dialyses the native reductants out. Do not dialyse the V2 lysate.

States: A soluble Au, E_r fresh sites, E_o spent sites, R carried-over reductant (finite, no regeneration), B Au(0).

vred=kredAEr  vFW=(k1+k2B)A  v=min(vred,vFW)

dAdt=−v dBdt=+v dErdt=−νv+vrech−koxEr dRdt=−νRvrech

vrech=krechEoR1+A/Ki

with ν=ne,Au/2: 0.5 for Au(I) (our feed), 1.5 for Au(III).

The slow step is nucleation, not electron transfer. Thiol+gold redox completes in ~100 s, but the observed process takes 8–48 h — a factor of ~300. k1 is nucleation (slow); k2B is autocatalytic growth, accelerating as surface accumulates.

### 4.1 Electron budget — the rate-free ceiling

ηreduce≤2Etot+2R0ne,AuA0

Needs no rate constant. At 5.78 µM Au(I), 0.2 g/L protein already supplies 98.9% of the electrons needed, so ηreduce≈1 on the budget.

The same arithmetic reproduces the source papers’ regime: at 2 mM Au(III) with 0.1 g/L protein the budget covers 0.048% — which is why they never measured conversion.

Regeneration does not decide the outcome. Sweeping krech over five orders and R0 over four leaves ηreduce at 97.7–100%. Even with zero regeneration, 97.7%. The carried-over reductant’s real role is buffering against aerobic inactivation (kox), not driving turnover.

Verification (all pass): fast-limit exponential decay (err 1.3e-09); stoichiometric limit B∞=Etot/ν exact; site conservation (6e-13); gold mass balance (2e-10).

### 4.2 The testable prediction

| t (h) | 1 | 2 | 4 | 8 | 12 | 24 |
| --- | --- | --- | --- | --- | --- | --- |
| η_reduce | 0.01% | 0.04% | 0.4% | 31% | 98% | 100% |

Sigmoid with a pronounced induction period. A non-nucleation model predicts monotone-decelerating decay — fastest at t=0. Opposite shapes in the first four hours.

Experiment: gold + lysate, sample 0/1/2/4/8/24 h, read A₅₂₀.

| observation | conclusion |
| --- | --- |
| little happens, then rapid conversion | nucleation-limited — confirmed |
| fastest at t=0, gradually slowing | electron-transfer-limited |
| never completes | budget- or reductant-limited |

⚠️ k1 and k2 are calibrated against one qualitative observation (“nanoparticles visible at 8 h”), checked only against a published gold F-W fit via the dimensionless shape group k2[A]0/k1 — ours 23,120 vs literature 10,685, a factor of 2.2. They are the joint #1 driver of the pipeline and are not measured.

## 5. Recovery (rung 11)

ηphys=ηspin⋅ηwash⋅ηash

Centrifugation, not gravity settling. Stokes (v∝r2, gold 19.3 g/cm³), time to fall 10 cm: 10 nm → 290 days; 100 nm → 3 days; 1 µm → 42 min. Nanoparticles never settle unaided.

⚠️ But centrifugation does not remove the size dependence. A commercial protocol reports ~50% recovery for 10 nm gold after a 30-minute size-matched spin.

| term | value | basis |
| --- | --- | --- |
| eta_spin | 0.50 (10 nm) – 0.97 (>200 nm) | sourced only at 10 nm |
| eta_wash | 0.95 | unsourced — upper bound |
| eta_ash | 0.98 | conditional on temperature ↓ |

Hard process constraint: ash at 500–600 °C, do not exceed. Biomass fully decomposes there and gold is retained. Above it, gold partially volatilises into the off-gas and recondenses in fine ash — in a lab furnace, on the walls.

### 5.1 The trade-off this creates

High protein → better conversion → smaller particles → worse recovery. ηreduce and ηphys pull against each other through protein loading. Rung 12 must optimise their product, not each separately. Particle-size distribution therefore re-enters the model.

### 5.2 Purity

Core is verified metallic fcc Au(0) (XRD Bragg reflections, SAED, EDX). Every particle carries a protein coat — the reducing protein is also the stabilising agent. The organic fraction has never been quantified; the obvious EDX measurement is confounded by the carbon TEM grid.

Purity scales with size (5 nm coat assumed): ~86% Au at 10 nm core, ~98% at 50 nm, ~99.5% at 200 nm. Calcination removes the remainder.

Context: the V2 output is 0.02–0.07% gold by mass — comparable to raw e-waste PCBs. The gain is form (discrete separable metal), not grade.

## 6. Optimisation

Two objectives, and they conflict. ηtotal is a fraction; maximising it starves the feed.

| Au_feed | ηtotal​ | Au recovered |
| --- | --- | --- |
| 3 µM | 63.1% | 1.89 µM |
| 10 µM | 59.2% | 5.92 µM |
| 50 µM | 24.8% | 12.41 µM |
| 100 µM | 10.8% | 10.77 µM |

Optimum A (maximise fraction): feed 10 µM, tharvest 16 h, tk 6 h.

| particle size | ηphys​ | ηtotal​ |
| --- | --- | --- |
| 10 nm (only sourced value) | 0.465 | 32.3% |
| 50 nm | 0.745 | 51.8% |
| >200 nm | 0.903 | 62.8% |

Optimum B (maximise absolute gold): feed 50 µM → 12.9 µM recovered, but that is where A_tox uncertainty is worst. Operate at 10–20 µM.

Lever behaviour: tharvest is flat (not an optimisation variable); tk has diminishing returns past 3/kmax; protein loading saturates for conversion at 0.2 g/L and worsens recovery above it; Au_feed dominates.

### 6.1 Where the losses are

At Optimum A, 10 µM feed, ϕ=0.13, ηphys=0.465:

| stage | efficiency | points lost |
| --- | --- | --- |
| recovery | 46.5% | 53.5 |
| capture | 79.9% | 20.1 |
| elution | 87.0% | 13.0 |
| reduction | 100.0% | 0.0 |

Recovery is the largest loss — and the least-modelled stage. If particles are large (>200 nm) the ranking reverts to capture-first, so it is contingent on a quantity nobody has measured.

## 7. Parameters

| symbol | value | status |
| --- | --- | --- |
| V1 |  |  |
| mu, Xmax, X0, m | 0.70, 5.0, 0.05, 0.005 | standard E. coli |
| q_max | 4.4 µM/(g/L), sweep 0.33–4.4 | ⚠️ may be 5–13× optimistic vs published display ceiling |
| K_D | 0.1 µM (conservative), sweep 1e-4–0.1 | insensitive (PRCC ≈0); bounded by CXXC proxies |
| k_on | 1.0 | unsourced; only K_D matters |
| A_tox | 250 µM (LB MIC), pessimistic 30 | LB regime; two sources agree on ~30 µM onset |
| k_dam, k_rep0 | 1.0, 0.1 | unsourced; k_dam/A_tox non-identifiable — only the ratio is determined |
| w | 1.0 | insensitive (PRCC −0.02) |
| Au_feed | 10–20 µM target | input from out-of-scope leaching model |
| Elution |  |  |
| phi | 0.13, sweep 0.05–0.30 | 87% desorption, protein biosorbent + 1 M thiourea. May be formulation-dependent (95–98% with additives) |
| k_max | 2.0 /h at 1 M thiourea | design lever via [TU] |
| Reduction |  |  |
| k_red | 0.0072–158 µM⁻¹h⁻¹, log | literature thiol-Au bracket; insensitive given F-W |
| k1, k2 | 5e-5 /h, 0.2 µM⁻¹h⁻¹ | weakly calibrated — joint #1 driver |
| k_ox | 0.02 /h | unsourced; measurable (air vs N₂) |
| k_rech, K_i | 0.1, 500 | insensitive |
| R0 | 10–1000 µM | lysis-dilution choice, not a literature value |
| nu | 0.5 (Au(I)) | stoichiometric |
| E_tot | protein/70000 × 1e6 | measurable; set by induction |
| Recovery |  |  |
| eta_spin | 0.45–0.99 | sourced only at 10 nm (~0.50) |
| eta_wash | 0.95 | unsourced — upper bound |
| eta_ash | 0.98 | conditional on 500–600 °C |

## 8. Uncertainty

Latin hypercube, n=3000, log-scale priors on rate constants, PRCC global sensitivity. Design variables are held at the optimum, not sampled.

| term | 5% | median | 95% |
| --- | --- | --- | --- |
| eta_capture | 15.0% | 53.5% | 100.0% |
| eta_elute | 51.6% | 69.3% | 87.4% |
| eta_reduce | 0.0% | 73.0% | 100.0% |
| eta_phys | 39.9% | 60.6% | 83.4% |
| ETA_TOTAL | 0.0% | 10.5% | 49.4% |

Report the interval, not the median. A point estimate built from many uncertain parameters lands wherever the favourable ends coincide.

PRCC: k2 +0.785, q_max +0.783, Xmax +0.370, k1 +0.366, ϕ −0.321, eta_spin +0.313, k_red +0.214. Insensitive (<0.05): K_D, K_i, k_on, k_max, w.

The 0.0% floor comes from slow-k1/k2 draws where reduction does not complete in 24 h. Only the §4.2 experiment closes it.

Re-run after any prior change — the interactions are the point:

from ensemble import sample, chain, prcc, NAMES
import numpy as np
X = sample(3000, seed=7); res = np.array([chain(r) for r in X])
print(np.percentile(res[:,4], [5,50,95]))

~75 s. PRCC ranks stable above ~2000 samples.

## 9. Measurement priority

- Reduction time course — gold + lysate, 0/1/2/4/8/24 h, A₅₂₀. Addresses k1+k2 (joint #1), tests model structure, and is the only route to closing the 0.0% floor. Also the only test of whether the chemistry works at all.

- q_max — display density. Being addressed by the secretion model.

- Conversion quantification (ICP-MS or colorimetric, not colour/TEM).

- ηspin and particle size on real product.

- Eluent confirmation — thiourea or acid-only.

- ηwash — last unsourced parameter.

## 10. What the model cannot tell you

Wet-lab facts: whether the construct reduces gold in lysate at all; what fraction of gold converts; selectivity against Cu/Ag/Ni in real leachate; whether GolB’s own Cys10/Cys13 oxidise shut during a 13 h aerobic run.

Structural gaps: Au_feed has no upstream model though it dominates V1; conditioning (V1→V2 transfer) is assumed lossless; particle-size distribution is absent though it now couples two η terms; k_dam/A_tox are structurally non-identifiable.

Open branch: incineration could replace elution entirely, deleting elution and conditioning, at the cost of destroying the biofilm.