# Bioleaching Modelling — Process Overview

Bacteria express tetrathionate hydrolase (TetH), which breaks tetrathionate down into thiosulfate. The thiosulfate then leaches gold (and, unavoidably, copper) from crushed PCB particles. The chain of models is:

- Enzyme production rate

- Tetrathionate consumption rate

- Thiosulfate production rate (with Cu(II) coupling)

- Gold leaching rate — Model A (oxygen only) and Model B (oxygen + Cu(II))

- Copper leaching rate and the Cu(I)/Cu(II) balance

- pH change (to be built)

## Enzyme Production

Bacteria produce tetrathionate hydrolase (TetH), which hydrolyses tetrathionate to thiosulfate.[1]

Reaction

bacteria  →  TetH enzyme (E)

Model

Enzyme concentration is governed by three processes — production (proportional to biomass), first-order degradation, and dilution as the cells grow [3]:

dEdt= ksyn·X  -  (kdeg+μ)·E

At steady state, [E]ₛₛ = k_syn·X / (k_deg + μ), reached over a characteristic time of 1/(k_deg+μ) [3]. Under the fixed-biomass assumption (no growth), μ = 0.

Parameters

| Symbol | Meaning | Unit | Value / source |
| --- | --- | --- | --- |
| [E] | Active TetH concentration | µmol L⁻¹ | state variable |
| t | Time | min | — |
| X | Biomass concentration | cell L⁻¹ | input / measured |
| k_syn | Enzyme synthesis rate per cell | µmol cell⁻¹ min⁻¹ | calibrate |
| k_deg | Enzyme degradation rate | min⁻¹ | ≈1.1×10⁻³ [4] |
| Μ | Growth-dilution rate (=ln2/t_double) | min⁻¹ | 0 if no growth [3] |

## Tetrathionate Consumption

Reactions

TetH hydrolyses tetrathionate via a disulfane-monosulfonic-acid (DSMSA) intermediate [1]:

S₄O₆²⁻ + H₂O  →  HS₂SO₃⁻ + HSO₄⁻

HS₂SO₃⁻  →  S₂O₃²⁻ + S⁰ + H⁺

Lumped into a single overall reaction:

S₄O₆²⁻ + H₂O  →  S₂O₃²⁻ + S⁰ + SO₄²⁻ + 2H⁺

Copper(II) leached from the PCB re-oxidises thiosulfate back to tetrathionate, so a regeneration term is required [6][7]:

2Cu(II) + 2S₂O₃²⁻  →  2Cu(I) + S₄O₆²⁻

Model

Consumption follows irreversible Michaelis–Menten kinetics [5]; the parasitic reaction above adds tetrathionate back:

dS4O62-dt= Fin-kcat·E·S4O62-Km+ S4O62-+ k₁·[Cu(II)]·[S₂O₃²⁻]

Parameters

| Symbol | Meaning | Unit | Value / source |
| --- | --- | --- | --- |
| [S₄O₆²⁻] | Tetrathionate concentration | µmol L⁻¹ | state variable |
| F_in | Tetrathionate feed rate | µmol L⁻¹ min⁻¹ | operating choice |
| k_cat | Turnover number of TetH | min⁻¹ | unmeasured — calibrate [1] |
| K_m | Michaelis constant | µmol L⁻¹ | 50–2400 [2] |
| E | Active TetH concentration | µmol L⁻¹ | from Section 1 |
| k₁ | Parasitic Cu(II)–thiosulfate rate constant | L µmol⁻¹ min⁻¹ | calibrate (↑ w/o NH₃) [6][7] |
| [Cu(II)] | Copper(II) concentration | µmol L⁻¹ | from Section 5 |

# Thiosulfate Production

Thiosulfate is produced as a stoichiometric multiple (Y) of tetrathionate consumed.

dS2O32-dt=kcat·E·S4O62-Km+ S4O62- [production only]

Adding the parasitic loss to Cu(II) (2 thiosulfate consumed per reaction extent) and the loss to gold leaching gives the full balance:

dS2O32-dt  =kcat·E·S4O62-Km+S4O62--2·k1·CuII·S2O32--2V·RAu-1V·RCu

where R_Au is the gold-leaching rate (µmol min⁻¹) and R_Cu is the copper-leaching rate (µmol min⁻¹) from Sections 4 and 5. Each gold atom consumes 2 thiosulfate, and, depending on the oxidant, each copper atom consumes 2 or 4 thiosulfate. The 1/V converts the surface rate to a concentration rate.

Parameters

| Symbol | Meaning | Unit | Value / source |
| --- | --- | --- | --- |
| [S₂O₃²⁻] | Thiosulfate concentration | µmol L⁻¹ | state variable |
| Y | Stoichiometric yield (S₂O₃ per S₄O₆) | — (dimensionless) | 1 [1] |
| V | Reactor volume | L | operating choice |
| R_Au | Gold leaching rate | µmol min⁻¹ | from Section 4 |
| R_Cu | Copper leaching rate | µmol min⁻¹ | From Section 5 |

# Gold Leaching

Reactions

Metallic gold is oxidised and complexed by thiosulfate. The oxidation and complexation happen in a single surface step (free Au⁺ does not persist in solution) [8]:

Au⁰ + 2S₂O₃²⁻  →  Au(S₂O₃)₂³⁻ + e⁻   (anodic half-reaction)

With oxygen as the terminal oxidant, the overall reaction is:

4Au⁰ + 8S₂O₃²⁻ + O₂ + 2H₂O  →  4Au(S₂O₃)₂³⁻ + 4OH⁻

Because copper is leached from the PCB, a second, faster pathway exists in which Cu(II) is the oxidant [11][12]:

Au⁰ + 2S₂O₃²⁻ + Cu(II)  →  Au(S₂O₃)₂³⁻ + Cu(I)

Gold Surface-Area Equation

Gold on a PCB is a thin plated film, not a bulk particle, so it dissolves by thinning at roughly constant face area until it is exhausted (it does not shrink inward). The exposed area is fixed by the gold mass and plating thickness, independent of how finely the board is crushed:

AAu =mAuρAu · tfilm

AAu (t) ≈ AAu(0)  while gold remains,   → 0 once exhausted

Derivation: a film of area A and thickness t has volume A·t = m/ρ, so A = m/(ρ·t).

### Model A — Oxygen only (conservative)

Starting from simple mass action, gold leaching depends on oxygen (oxidant) and thiosulfate (ligand). Because gold sits on the particle surface, the rate scales with a time-dependent gold area — a shrinking-surface variant of the shrinking-core model

Since the surface has a finite number of reaction sites, each reactant enters through a saturating (Langmuir) term [8][10]. Tracking solid gold in mol and dissolved gold as a concentration:

RAu = kAu,O2· AAu(t)·O2KO2+O2 ·S2O32-KS+S2O32-

dnAudt= - RAu

dAuS2O323-dt=+RAuV

### Model B — Oxygen + Copper(II) (realistic)

Cu(II) provides a parallel oxidant pathway. Parallel pathways add (either oxidant alone can dissolve gold), while area, thiosulfate, and passivation multiply everything (all are required regardless of oxidant). Oxygen enters only its own term — Cu(II) does not need O₂ at the gold surface [15]:

RAu = AAu(t)·S2O32-KS+S2O32-  · {kAu,O2·O2KO2+O2 + kAu,Cu·CuIIKCu+CuII }

dnAudt = -RAu

dAuO33-dt = +RAuV

Parameters

| Symbol | Meaning | Unit | Value / Source |
| --- | --- | --- | --- |
| n_Au | Solid gold remaining | mol (or µmol) | state variable |
| [Au(S₂O₃)₂³⁻] | Dissolved gold complex (product) | µmol L⁻¹ | state variable |
| A_Au | Exposed gold area = m_Au/(ρ_Au·t_film) | m² | from geometry |
| ρ_Au | Gold density | kg m⁻³ | 19300 |
| t_film | Gold plating thickness | M | 0.05–1 ×10⁻⁶ (board spec) |
| k_Au,O₂ | Gold rate constant, O₂ route | µmol m⁻² min⁻¹ | ≈11 (1.9×10⁻⁷ mol m⁻²s⁻¹) [9][10] |
| k_Au,Cu | Gold rate constant, Cu(II) route | µmol m⁻² min⁻¹ | ≈10³× larger [11][12] |
| K_O₂ | O₂ half-saturation | µmol L⁻¹ | calibrate (~50) |
| K_S | Thiosulfate half-saturation | µmol L⁻¹ | calibrate (~5×10⁴) |
| K_Cu | Cu(II) half-saturation | µmol L⁻¹ | Calibrate |

## Copper Leaching and the Cu(I)/Cu(II) Balance

Reactions

Metallic copper dissolves as Cu(I)–thiosulfate. Two oxidant pathways exist [13][7]:

With oxygen as oxidant:

4Cu⁰ + O₂ + 8S₂O₃²⁻ + 2H₂O  →  4[Cu(S₂O₃)₂]³⁻ + 4OH⁻

With Cu(II) as oxidant (comproportionating one Cu(II) plus one Cu⁰ gives two Cu(I)):

Cu⁰ + Cu²⁺  →  2Cu⁺

Cu⁺ + 2S₂O₃²⁻  →  [Cu(S₂O₃)₂]³⁻

Cu⁰ + Cu²⁺ + 4S₂O₃²⁻  →  2[Cu(S₂O₃)₂]³⁻

Cu(I) is re-oxidised to Cu(II) by oxygen, and Cu(II) is reduced back to Cu(I) by thiosulfate and by gold leaching [7][15]:

4Cu(I) + O₂ + 2H₂O  →  4Cu(II) + 4OH⁻

2Cu(II) + 2S₂O₃²⁻  →  2Cu(I) + S₄O₆²⁻

Au⁰ + 2S₂O₃²⁻ + Cu(II)  →  Au(S₂O₃)₂³⁻ + Cu(I)

Copper Surface-Area Equation

Copper is bulk metal (traces, planes, inner layers), so its particles genuinely erode inward — a true shrinking-particle geometry

The initial area follows the surface-to-volume ratio 6/d for crushed particles of size d; as copper is consumed, the area falls as the two-thirds power of the fraction remaining (area ∝ r², volume ∝ r³) [14]:

ACu0= 6·mCu(ρCu · d)

ACu(t) = ACu(0) · nCunCu023

Rates

Copper leaching, oxygen route (v₁A) and combined-oxidant route (v₁B); gold-leaching Cu(I) return (v₂); parasitic tetrathionate regeneration (v₃); Cu(I) re-oxidation by oxygen (v₄):

v1A = 2kCu,O2·ACut·O2KO2+O2·S2O32-KS+S2O32-

v1B = ACu(t)·S2O32-KS+S2O32-·{ 2kCu,O2·O2KO2+O2 + 4kCu,  Cu2+·CuIIKCu+CuII }

v₂ = RAu  (gold-leaching rate, Section 4)

v₃ = k₃·[Cu(II)]·[S₂O₃²⁻]

v₄ = k₄·[O₂]·[Cu(I)]

Cu(I) model

Cu(I) is produced by copper leaching, by gold leaching, and by the parasitic reaction, and is consumed by oxygen re-oxidation. Reading coefficients off the balanced reactions (comproportionating gives 2 Cu(I) per extent; parasitic gives 2 Cu(I) per extent; O₂ re-oxidation consumes 4 Cu(I) per extent):

dCuIdt = 1V·2·v₁B + 1V·v₂ + 2·v₃ - 4·v₄

Cu(II) model

Cu(II) is produced only by oxygen re-oxidation of Cu(I), and consumed by the comproportionating leach, the parasitic reaction, and gold leaching:

dCuIIdt = 4·v₄ - 1V·v₁B - 1V·v₂ - 2·v₃

Parameters

| Symbol | Meaning | Unit | Value / source |
| --- | --- | --- | --- |
| [Cu(I)] | Copper(I) concentration (cannot leach gold) | µmol L⁻¹ | state variable |
| [Cu(II)] | Copper(II) concentration (gold oxidant) | µmol L⁻¹ | state variable |
| n_Cu | Solid copper remaining | mol | state variable |
| A_Cu | Exposed copper area = 6m_Cu/(ρ_Cu·d)·(n/n₀)^⅔ | m² | from geometry |
| ρ_Cu | Copper density | kg m⁻³ | 8960 |
| d | Crushed particle size | m | 2–6×10⁻³ (your feed) |
| k_Cu,O₂ | Copper rate constant, O₂ route | µmol m⁻² min⁻¹ | calibrate (Ea≈25.8 kJ/mol) [13] |
| k_Cu,Cu | Copper rate constant, Cu(II) route | µmol m⁻² min⁻¹ | calibrate |
| k₃ | Parasitic (Cu(II)+S₂O₃) rate constant | L µmol⁻¹ min⁻¹ | ≈ k₁ [6][7] |
| k₄ | Cu(I) re-oxidation rate constant | L µmol⁻¹ min⁻¹ | calibrate |

# References

[1] Y. Kanao et al., "Tetrathionate hydrolase from the acidophilic microorganisms," Front. Microbiol., vol. 15, 1338669, 2024.

[2] Y. Kanao, K. Kamimura, and T. Sugio, "Purification of a tetrathionate hydrolase from Acidithiobacillus ferrooxidans," J. Biotechnol., vol. 132, pp. 16–22, 2007.

[3] U. Alon, An Introduction to Systems Biology, 2nd ed. Boca Raton, FL: CRC Press, 2019.

[4] M. R. Maurizi, "Proteases and protein degradation in Escherichia coli," Experientia, vol. 48, pp. 178–201, 1992.

[5] G. E. Briggs and J. B. S. Haldane, "A note on the kinetics of enzyme action," Biochem. J., vol. 19, pp. 338–339, 1925.

[6] J. J. Byerley, S. A. Fouda, and G. L. Rempel, "Kinetics and mechanism of the oxidation of thiosulphate ions by copper(II) ions in aqueous ammonia solution," J. Chem. Soc. Dalton Trans., pp. 889–893, 1973.

[7] P. L. Breuer and M. I. Jeffrey, "The reduction of copper(II) and the oxidation of thiosulfate and oxysulfur anions in gold leaching solutions," Hydrometallurgy, vol. 70, pp. 163–173, 2003.

[8] G. Senanayake, "Analysis of reaction kinetics, speciation and mechanism of gold leaching and thiosulfate oxidation by ammoniacal copper(II) solutions," Hydrometallurgy, vol. 75, pp. 55–75, 2004.

[9] S. Zhang and M. J. Nicol, "An electrochemical study of the dissolution of gold in thiosulfate solutions Part I: Alkaline solutions," J. Appl. Electrochem., vol. 33, pp. 767–775, 2003.

[10] O. Sitando et al., "A review of factors affecting gold leaching in non-ammoniacal thiosulfate solutions," Hydrometallurgy, vol. 178, pp. 151–175, 2018.

[11] M. G. Aylmore and D. M. Muir, "Thiosulfate leaching of gold — a review," Miner. Eng., vol. 14, no. 2, pp. 135–174, 2001.

[12] D. Maharaj, T. Moyo, and J. Petersen, "Ammonium thiosulfate leaching of gold from electronic printed circuit boards — effect of solution copper concentration," J. S. Afr. Inst. Min. Metall., vol. 124, no. 12, pp. 711–718, 2024.

[13] E. Salinas-Rodríguez et al., "Leaching of copper contained in waste printed circuit boards using the thiosulfate–oxygen system: a kinetic approach," Materials, vol. 15, no. 7, 2354, 2022.

[14] O. Levenspiel, Chemical Reaction Engineering, 3rd ed. New York, NY: Wiley, 1999.

[15] P. L. Breuer and M. I. Jeffrey, "The effect of ionic strength and buffer choice on the decomposition of tetrathionate; and the role of copper(II) as oxidant in gold thiosulfate leaching," Hydrometallurgy, vol. 65, pp. 145–157, 2002.